## Slide 1: High Temperature Structural Products, Improved Performance at Elevated Temperatures and Harsh Environments
Matt Torosian,
Product Manager, High Temperature Structural Products

## Slide 2: Presentation Overview
What are Ultra Performance products?
Highlights
Review of competing materials
  Metals
  Conventional engineering thermoplastics
  VLF Products
    Vs. Conventional reinforced TP compounds
Notes: See next slide for comments…

## Slide 3: Ultra Performance Structural
Dictionary: "Ultra” - Very or extreme. (descriptive)
Short Glass Fiber
Short Carbon Fiber
Very Long Glass Fiber (VLF)
PEEK
PPA
PPS
PEI
Ultra Performance
Structural Compounds

## Slide 4: Ultra Performance Structural
Built upon RTP Company’s current standard product portfolio of industry-leading reinforced compounds by
Optimizing reinforcement technology
Optimizing process technology
Ultra Performance structural products are in addition to and do not replace our current high temperature structural products

## Slide 5: Ultra Performance Highlights
10-30% higher strength and modulus in the RTP Company high temperature portfolio.
  Greatest gains in CF compounds
PPA and PPS w/CF demonstrate a 30-40% improvement in room temperature physical properties.
40%CF PEEK with exceptional properties Vs. Victrex 90 HMF 40, the only other High Modulus PEEK available.
  Targeted metal replacement in energy and D&A
VLF products have 3-4 times the impact of short glass products
  Improved creep, fatigue and CLTE
5. Technology is transferable to other polymer
systems

## Slide 6: Ultra Performance Structural Compounds for Greene Tweed, Houston TX

## Slide 7: Ultra Performance Structural
Competitive metals
Die cast aluminum
Heat treated T-6 aluminum
Die cast zinc alloy (Zamak 3)

## Slide 8: Competitive Materials
A-380 die cast aluminum and 6061 T-6 heat treated aluminum
  A-380 accounts for over 85% of the Al die cast market
Pros
  Excellent high temperature performance
  Very good thermal conductivity
  Very good EMI shielding capabilities
  Good corrosion resistance
  Light: good strength-to-weight ratio (specific strength)
Cons
  Poor chemical resistance
  Poor fatigue resistance
  Subject to attack by galvanic corrosion when in contact with carbon fiber, carbon fiber composites, and other metals

## Slide 9: Competitive Materials
ZAMAK alloys are widely used in die casting
Pros
  Very good EMI shielding
  Very good conductivity
  Good strength
Cons
  Poor creep resistance under load
  Poor strength-to-weight ratio
  Difficult to process vs. injection moldable plastics

## Slide 10: ISO Tensile Strength
Chart: ISO Tensile Strength
| Zamak 3 | AL 6061 T-6 | AL - A380 | RTP 2287 UP | RTP 4087 UP
Tensile | 283 | 310 | 325 | 305 | 360
PEEK CF
PPA CF
Heat Treated AL
Die Cast AL
ZAMAK 3

## Slide 11: Specific Tensile Strength
Chart: 
| RTP 4087 UP | RTP 1387 UP | RTP 2287 UP | RTP 2187 UP | AL A 380 | Al 6061 T6 | Zamak 5
Specific Strength | 189.0359 | 118.6998 | 143.085 | 124.7005 | 75.9259 | 82.3045 | 55.7576
Specific gravity | 1.38 | 1.48 | 1.46 | 1.43 | 2.7 | 2.7 | 6.6
N·mm/kg
g/cc

## Slide 12: What about Tg and Tm
Tg or glass transition temperature is critical when comparing materials for High Temp applications
  Conventional semi-crystalline thermoplastics are usable above their Tg but physical properties begin to deteriorate quickly
  Amorphous materials have defined Tg but have a more gradual drop off in properties bellow the Tg(see graph)
Creep and fatigue have increased effects above the TG of thermoplastic materials
  Crystallinity is critical and affects the Tg
  End use testing is the best measure of performance

## Slide 13: Tensile Strength @ Temperature
Chart: MPa
| 23.0 | 120.0 | 150.0 | 175.0 | 200.0
RTP 2209 UP | 208 | 150.4964 | 111.9023 | 73.3339 | 52.7014
RTP 2109 UP | 179 | 144.465 | 98.9634 | 87.6412
RTP 4009 UP | 223.3521 | 174.9761 | 110.7175 | 93.3398 | 76.6087
RTP 1309 UP | 197 | 168 | 135 | 100 | 62
°C
Notes: Tg has a significant affect on high temperature performance. Note the significant drop in Tensile Strength at the Tg of Crystalline systems and the more gradual softening and decay in properties of the amorphous PEI.

## Slide 14: Ultra Performance Structural Compounds vs. Competitive Thermoplastics

## Slide 15: PPA 40%CF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flex Modulus | Notched Izod Impact
PPA 40% CF Comp | 0.64444 | 0.85542 | 0.73276 | 0.77101 | 0.81111
RTP 4087 | 0.76389 | 0.78313 | 0.71552 | 0.7971 | 0.77778
RTP 4087 UP | 1 | 1 | 1 | 1 | 1

## Slide 16: Data Table of Ultra Performance PPA
Material | RTP 4087 | RTP 4087 UP | Comp. PPA 40% CF | 
Tensile Strength | 275 | 360 | 232 | MPa
Tensile Modulus | 32500 | 41500 | 35500 | MPa
Flexural Strength | 415 | 580 | 425 | MPa
Flexural Modulus | 27500 | 34500 | 26600 | MPa
Notched Izod Impact, | 7.0 | 9.0 | 7.0 | KJ/m²
Note: Properties tested using ISO test methods

## Slide 17: PPS 40%CF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flex Modulus | Notched Izod Impact,
PPS 40% CF Comp. | 0.79615 | 0.85185 | 0.51605 | 0.92308 | 0.93333
RTP 1387 | 0.82692 | 0.83951 | 0.7284 | 1 | 0.66667
RTP 1387 UP | 1 | 1 | 1 | 1 | 1

## Slide 18: Data Table of Ultra Performance PPS
Material | RTP 1387 | RTP 1387 UP | Comp. PPS 40% CF | 
Tensile Strength | 215 | 260 | 207 | MPa
Tensile Modulus | 34000 | 40500 | 34500 | MPa
Flexural Strength | 295 | 405 | 209 | MPa
Flexural Modulus | 32500 | 32500 | 30000 | MPa
Notched Izod Impact, | 5.0 | 7.5 | 9.0* | KJ/m²
Note: Properties tested using ISO test methods
* Competitive material is a PPS alloy (no other 40% CF PPS competitive data available)

## Slide 19: PEEK 40%CF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flexural Modulus | Notched Izod Impact,
RTP 2287 HF | 0.8871 | 0.78261 | 0.86458 | 0.79487 | 0.6
RTP 2287 UP | 0.98387 | 0.86957 | 0.97917 | 0.87179 | 0.7
RTP 2299 X 133017 | 1 | 1 | 1 | 1 | 1
PEEK Comp. HM CF | 1.0645 | 0.97826 | 1 | 0.94872 | 1.1

## Slide 20: Data Table of Ultra Performance PEEK
Material | RTP 2287 HF | RTP 2287 UP | RTP 2299 X 133017 | Comp. PEEK 40% CF | 
Tensile Strength | 270 | 275 | 310 | 330 | MPa
Tensile Modulus | 27500 | 36000 | 46200 | 45000 | MPa
Flexural Strength | 385 | 415 | 480 | 480 | MPa
Flexural Modulus | 24000 | 31000 | 39300 | 37000 | MPa
Notched Izod Impact, | 6.5 | 6 | 10 | 11 | KJ/m²
Note: Properties tested using ISO test methods

## Slide 21
An Introduction to VLF – Very Long Fiber Composites in High Temperature Materials

## Slide 22: Typical Long Fiber Pellets

## Slide 23: Short Fiber & VERY LONG FIBER
3 mm
12 mm
Fibers: ~2 mm 12 mm

## Slide 24
PA 66 + 60% VLF
Seat Belt Tensioner Housings
The Structural Skeleton

## Slide 25
Additives
Your color – Your way™
Flame retardants
Wear & lubricity
Heat stabilizers
Nano particles
UV resistance
Conductivity
Anti-stat
Polymers
PEEK
PPS
PBT
TPU
PP
PA
“Long Cut” technology
Glass
Carbon
Steel
Masterbatch VLF Technologies

## Slide 26: PEI 40%GF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flex Modulus | Notched Izod Impact,
PEI 40% GF Comp.. | 0.87805 | 0.7931 | 0.84211 | 0.71429 | 0.88889
VLF 82107 | 0.95122 | 0.96552 | 0.96491 | 1 | 2.1111
RTP 2107 | 0.92683 | 0.96552 | 0.96491 | 0.92857 | 1
RTP 2107 UP | 1 | 1 | 1 | 1 | 1

## Slide 27: PPS 50%GF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flex Modulus | Notched Izod Impact,
PPS 50% GF Comp. | 1 | 0.9 | 0.91525 | 0.86486 | 0.80952
VLF 81309 | 0.87179 | 0.925 | 0.98305 | 1 | 2.381
RTP 1309 | 0.87179 | 0.925 | 0.79661 | 0.97297 | 0.80952
RTP 1309 UP | 1 | 1 | 1 | 1 | 1

## Slide 28: PPA 50%GF Relative Properties
Chart: 
| Tensile Strength | Tensile Modulus | Flex Strength | Flex Modulus | Notched Izod Impact,
PPA 50% GF Comp. | 0.94737 | 0.85 | 0.88636 | 0.91892 | 0.66667
VLF 84009 | 0.96491 | 0.9 | 0.90909 | 0.97297 | 2.3333
RTP 4009 | 0.87719 | 0.9 | 0.84091 | 0.91892 | 0.66667
RTP 4009 UP | 1 | 1 | 1 | 1 | 1

## Slide 29: PPA 50%GF Actual Properties
 | PPA 50% GF Competitive | VLF 84009 50% VLF GF | RTP 4009 50% GF | RTP 4009 UP 50% UP GF | Units
Tensile Strength | 270 | 275 | 250 | 285 | MPa
Tensile Modulus | 17000 | 18000 | 18000 | 20000 | MPa
Flex Strength | 390 | 400 | 370 | 440 | MPa
Flex Modulus | 17000 | 18000 | 17000 | 18500 | MPa
Notched Izod Impact, | 10 | 35 | 10 | 15 | KJ/m²
Note: Properties tested using ISO test methods

## Slide 30: Questions?
Matt Torosian
mtorosian@rtpcompany.com
+1 317-663-4364